## Slide 1
有機分子のアセチリド化によるナノワイヤー作成：
各種置換基の影響と機能性分子のナノワイヤー化
明星大理工 〇西條純一，和田友明，石崎真也，若杉崇志，
奥山隼斗，坂下大樹，佐々木一樹

## Slide 2
Introduction

## Slide 3
Nanowires are attractive candidates for
many applications such as...
・Wiring material
・Catalyst support
・Anti-bacterial coating
・Medical-diagnosis
・Optical material etc.

## Slide 4
At the same time, the application of nanowires has been limited by the difficulties in the preparation.
Desirable preparation method:
・Facile and Mass-productive
→ Self-assembly is suitable
・Applicable for various materials
We focused on "Ag- and Cu-acetylides"
(M-CC-R)
Notes: 1分弱

## Slide 5
Why Ag/Cu acetylide?
1. Extremely anisotropic crystal structures
in the case of M-C≡C-Ph
Ag-C≡C-Ph
Cu-C≡C-Ph
powder XRD, S.S.Y. Chui et al., Chem. Eur. J., 1739 (2005).
Quite thin and long needle crystal (= nanowire)
J. Nishijo et al., Chem. Mater., 19, 4627-4629 (2007).
Notes: 2分弱

## Slide 6
Why Ag/Cu acetylide?
2. Small contribution of phenyl group to the structures
M-C≡C-R is likely to grow into nanowires
regardless of terminal functional groups.
Anisotropic structure is mainly originated from the metal cations and ethynyl groups.
Notes: 3分弱

## Slide 7
In short...
various organic molecules (R)
R-C≡C-H
introduction of an ethynyl group
Cu+ / Ag+ (acetylide)
Nanowires
Versatile method to construct nanowires
Notes: 3分15秒

## Slide 8
The aim of this study:
Is this method really "versatile"?
Elucidate the limitation of the applicability
Notes: 4分弱

## Slide 9
Experimental

## Slide 10
1. Preparation of acetylides
AgNO3 or CuCl: 6 mmol
R-C≡C-H: 7-8 mmol
Et3N (base): 7-8 mmol
CH3CN (solvent): 50 ml
Stir 12-24 h, then filtered.
Washed with CH3CN
(and MeOH).
SEM observation
Recrystallization
If not nanowire
SEM
Notes: 4分30秒

## Slide 11
2. Recrystallization
Most of the obtained acetylides are insoluble.
Therefore, we convert them into soluble complexes, followed by reprecipitation caused by dilution.
[M-C≡C-R]∞
[Me3P-M-C≡C-R]
[M-C≡C-R]∞
(insoluble)
(soluble)
(insoluble)
PMe3
-PMe3
dilute
1 m
1 m
Ag-C≡C-Ph (AS prepared)
Ag-C≡C-Ph (recrystallized)
Notes: 5分30秒

## Slide 12
Results and Discussion
(applicability of the method)

## Slide 13
200 nm
Cu (AS)
1-hexyne (Cu: Nanowire, Ag: Shapeless)
Diameter:
60 ± 14 nm
Ag (AS)
5 m
Length:
several m
*Recrystallization did not give
Ag-1-hexyne nanowire
Cu
Notes: 6分30秒

## Slide 14
m-fluorophenylacetylene (Cu, Ag: nanowire)
Cu (AS), nanorod
500 nm
500 nm
Cu, nanowire(?),
MeOH+EtOH
1 m
Ag (AS), nanowire
Diameter:
127 ± 40 nm
Length:
～5 m
Ag
Notes: 7分

## Slide 15
m-chlorophenylacetylene (Cu, Ag: nanowire)
Diameter:
41 ± 8 nm
Length:
few m
1 m
Cu (AS), nanowire
1 m
Ag (AS), nanowire
Diameter:
69 ± 16 nm
Length:
1-3 m
Ag
Cu
Notes: 7分30秒

## Slide 16
2-ethynylpyridine (Cu, Ag: nanowire)
Cu (AS), shapeless
1 m
Ag (AS), small plate
10 m
5 m
Ag, Nanowire, hexane
Diameter:
98 ± 28 nm
Length:
5-10 m
Ag
*Recrystallization did not give
Cu-2-ethynylpyridine nanowire.
Notes: 8分

## Slide 17
Ag (AS), small plate
10 m
p-ethynyltoluene (Cu: nanorod, Ag: nanowire)
Cu (AS), nanorod
500 nm
Diameter:
165 ± 42 nm
Length:
10-20 m
Ag
Diameter:
32 ± 7 nm
Length:
～500 nm
Cu
Ag, nanowire, 1-PrOH
1 m
Notes: 8分30秒

## Slide 18
Ag (AS), nanorod
500 nm
p-tertBu-phenylacetylene (Cu, Ag: nanowire)
Cu (AS), nanowire
1 m
1 m
Ag , nanowire, acetone
Length:
5～30 m
Diameter:
81 ± 27 nm
Ag
Length:
5～10 m
Diameter:
84 ± 22 nm
Cu
Notes: 9分

## Slide 19
p-ethnylhexylbenzene (Cu: shapeless, Ag: nanowire)
Cu (AS), shapeless
100 m
*Recrystallization did not give
Cu-p-ethynylhexylbenzene
nanowire.
Ag (AS), nanowire
3 m
Length:
5～15 m
Diameter:
250 ± 58 nm
Ag
Notes: 9分20秒

## Slide 20
4-ethnylbiphenyl (Cu, Ag: nanowire)
Cu (AS), nanowire
500 nm
Ag (AS), nanowire
1 m
Length:
few m
Diameter:
46 ± 11 nm
Length:
～1 m
Diameter:
38 ± 10 nm
Cu
Ag
Notes: 9分40秒

## Slide 21
Phenyl propargyl sulfide (Cu: nanorod, Ag: decomp.)
Cu (AS), shapeless
10 m
Length:
～1 m
Diameter:
92 ± 22 nm
Cu
5 m
500 nm
CHCl3 + toluene
Notes: 10分

## Slide 22
p-ethnylaniline (Cu: partially nanowire, Ag shapeless)
Cu (AS)
10 m
2 m
Ag (AS)
1 m
*We failed to recrystallize
these complexes.
Notes: 10分20秒

## Slide 23
5-hexyne-1-ol (Cu: nanorod?, Ag partially nanowire)
Ag (AS)
20 m
Ag (AS)
3 m
Cu (AS)
1 m
*We failed to recrystallize
these complexes.
Notes: 10分40秒

## Slide 24
4-pentyne-2-ol (Cu, Ag: fused nanowire)
Cu (AS)
2 m
Ag (AS)
10 m
The complexes are essentially
nanowire, but they are melt and fused.
*We failed to recrystallize
these complexes.
Notes: 11分

## Slide 25
1-ethynyl-1-cyclohexanol (Cu, Ag: shapless)
50 m
Cu (AS), shapeless
10 m
Ag (AS), shapeless
*We failed to recrystallize these complexes.
6-chloro-1-hexyne (Cu, Ag: decomposed)
1-diethylamino-2-propyne (Cu, Ag: decomposed)
Notes: 11分20秒

## Slide 26
Nanowire
Nanorod
Partially nanowire/nanorod
Decomposed
Shapeless nanoparticle
Notes: 12分

## Slide 27
Is it possible to prepare
functional nanowires by this method?

## Slide 28
Organic radical
(magnetic)
Fluorescent
Notes: 12分

## Slide 29
Results and Discussion 2
(functional nanowires)

## Slide 30
1. Organic radical (4-ethynyl-1-phenyl-NN)
Cu(recryst.), CH3CN
2 m
1 m
Ag (recryst.), CH2Cl2+Et2O
Length:
5-20 m
Diameter:
145 ± 48 nm
Cu
Notes: 12分30秒

## Slide 31
Magnetic susceptibility
One spin per one ligand
T  0.375 emu K /mol
(at high temperature)
Magnetic
Nanowire
Notes: 12分50秒

## Slide 32
2. Fluorescent molecule (9-Ethynylphenanthrene)
Cu (recryst.), hexane
500 nm
Ag (recryst.), hexane
1 m
Length:
1-3 m
Diameter:
90 ± 18 nm
Length:
1～2 m
Diameter:
65 ± 15 nm
Cu
Ag
Notes: 13分20秒

## Slide 33
Fluorescence
Cu complex: fluorescent
(Ag complex is not fluorescent)
Vis
UV
Emission wavelength
Excitation wavelength
Fluorescent Nanowire
Notes: 13分50秒

## Slide 34
Notes: 14分10秒

## Slide 35
Conclusion

## Slide 36
Nanowire
Nanorod
Partially nanowire/nanorod
Decomposed
Shapeless nanoparticle
Notes: 14分30秒

## Slide 37
・The present method was successful in producing nanowires from various organic molecules.
"Versatile method to construct nanowires"
・The existence of an aromatic ring probably promotes the formation of nanowires.
・Hydroxyl group and nitrogen atom may hinder the formation of nanowires.
 coordination affect a crystal structure?
Conclusion 1: Applicability of the method
Notes: 14分50秒

## Slide 38
Conclusion 2: Construct functional nanowires
・The present method is applicable to large and functional molecules such as nitronyl-nitroxide and phenanthrene.
・The functions of the molecules are maintained even in the nanowires.
New method to construct functional nanowires
Notes: 15分10秒

## Slide 39
Acknowledgement
We are grateful to Dr. M. Enomoto (Tokyo Univ. of Sci.) for his cooperation in the magnetic measurements.
Notes: 15分30秒